## Slide 1: Probability of Detection: Evaluating the Reliability of Nondestructive Inspection Systems
Christine Knott, PhD, Research Mathematician
AFRL/RXNW, Material state awareness branch

## Slide 2: Agenda
Background
Statistical Analysis
Designing the Experiment
Example: XCT for AM

## Slide 3: Evolution of Aircraft Structural Integrity
1903: Wright Brothers’ Static Loads Tests
During WWII, fatigue rarely seen
1956: Air Force structural integrity through Safe-Life
  Service Life Capability: “the total number of operating hours of the specific mission spectrum through which an aircraft structure has been determined by test and analysis to be capable of operating safely and economically,”
Cold War Era Losses
  1958: B-47 medium-range strategic bomber for nuclear deterrence
    Designed for high-altitude, used for low-altitude: fast pull-up, more weight, frequent take-off/landings
    Lost five B-47s in March and April of 1958 in midair - 4 had structural fatigue failure
  1969: F-111A fighter bomber and F-5 fighter - fatigue-related accidents well before end of safe-life
Damage Tolerant Design
  Assume aircraft have pre-existing manufacturing defects
  Safety through design, nondestructive inspection and maintenance

## Slide 4: Damage Tolerant Design Goal: multiple nondestructive inspection opportunities on critical structures before failure
Safety Risk
Expensive (Time/Money)
Unavailable for Mission
Inspection Frequency
Optimal
Too Infrequent
Too Frequent
FLIGHT HOURS
0 600 1200
=NDI Capability Limit
=Critical Flaw Size (Part Failure)
=Initial Flaw Size
RISK OF FAILURE
Initial Inspection
In-service Inspections
Flaw Growth Curve

## Slide 5: Probability of Detection: What is the largest defect size a nondestructive inspection system may miss?
DOE Goal: Understand capabilities of a specific NDE/NDI system for a specific application
Design an experiment which varies over all the known variables
Create specimens which represent the specific application
  Embed the appropriate kinds of defect/flaw/crack in some of the specimens
  Measure the size of the created defects
Perform round-robin study
  Specimens taken to several inspection locations
  Inspectors use the inspection system to gather data without knowing which specimens contain flaws.
Collected experiment data is analyzed using Statistical Models
  1. False Positive Rate checked
  2. Crack data (True Positives + False Negatives) analyzed using POD Methods
Results provide inputs to damage tolerant design calculations of inspection intervals
 | Flaw Detected | No Flaw Detected
Flaw Exists | True Positive | False Negative
No Flaw Exists | False Positive | True Negative
Probability of Detection
POD studies provide helpful inputs to decision-makers, but engineering judgement is still necessary.

## Slide 6: Agenda
Background
Statistical Analysis
Designing the Experiment
Example: XCT for AM

## Slide 7: Picking the inspection interval depends on the analysis of a designed experiment over all the important variables
Input Variables
  Defect Size
  People
  Part
  Probe
Notes: S.K. Bhaumik, M. Sujata, M.A. Venkataswamy, Fatigue failure of aircraft components, Engineering Failure Analysis, Volume 15, Issue 6, 2008, Pages 675-694, ISSN 1350-6307, https://doi.org/10.1016/j.engfailanal.2007.10.001. (https://www.sciencedirect.com/science/article/pii/S1350630707001409)
NIST Advanced Manufacturing Series 100-16 Literature Review of Metal Additive Manufacturing Defects Felix H. Kim Shawn P. Moylan Engineering Laboratory May 2018

## Slide 8: Picking the inspection interval depends on the analysis of a designed experiment over all the important variables
Input Variables
  Defect Size
  People
  Part
  Probe
Surface cracks
Internal Cracks
Corner Cracks
Notches
Corrosion
Pores
Delamination
Notes: S.K. Bhaumik, M. Sujata, M.A. Venkataswamy, Fatigue failure of aircraft components, Engineering Failure Analysis, Volume 15, Issue 6, 2008, Pages 675-694, ISSN 1350-6307, https://doi.org/10.1016/j.engfailanal.2007.10.001. (https://www.sciencedirect.com/science/article/pii/S1350630707001409)
NIST Advanced Manufacturing Series 100-16 Literature Review of Metal Additive Manufacturing Defects Felix H. Kim Shawn P. Moylan Engineering Laboratory May 2018
CNDE https://www.nde-ed.org/NDETechniques/MagParticle/Indications/WetExamples.xhtml

## Slide 9: Picking the inspection interval depends on the analysis of a designed experiment over all the important variables
Input Variables
  Defect Size
  People
  Part
  Probe
Different levels of experience
Different areas of experience

## Slide 10: Picking the inspection interval depends on the analysis of a designed experiment over all the important variables
Input Variables
  Defect Size
  People
  Part
  Probe
    Material(s)
    metal
    composite
    Geometry
    flat plate
    bolt hole
    Fastener head
    Joint
    fins
Notes: S.K. Bhaumik, M. Sujata, M.A. Venkataswamy, Fatigue failure of aircraft components, Engineering Failure Analysis, Volume 15, Issue 6, 2008, Pages 675-694, ISSN 1350-6307, https://doi.org/10.1016/j.engfailanal.2007.10.001. (https://www.sciencedirect.com/science/article/pii/S1350630707001409)

## Slide 11: Picking the inspection interval depends on the analysis of a designed experiment over all the important variables
Input Variables
  Defect Size
  People
  Part
  Probe
Magnetic Particle
Radiography
Florescent Penetrant
Ultrasound
Eddy Current
  Probe characteristics
  frequency
  field of view
  fixtures
  Calibration procedure
  how often?
  Noise
  electrical noise
  signal-to-noise
Notes: CNDE (https://www.nde-ed.org/NDETechniques/Ultrasonics/MeasurementTech/beaminspection.xhtml) and CNDE https://www.nde-ed.org/NDETechniques/MagParticle/Indications/WetExamples.xhtml

## Slide 12: Agenda
Background
Statistical Analysis
Designing the Experiment
Example: XCT for AM

## Slide 13: Probability of Detection Steps
Build a model relating NDI sensor response to defect size.
Transform model to a probability (of detection) curve.
Estimate a 95% confidence interval on the probability curve.
Probability of Detection Curve
95% Confidence Interval Curve
90% Probability of Detection
a90/95
a90

## Slide 14: The nondestructive evaluation system can provide categorical or continuous responses
Y = Response
X = Defect Size (a)
Signal-Response
Inspector Call
Detection = Hit
No Detection = Miss
Hit/Miss
X = Defect Size (a)
Response Variable
Notes: S.K. Bhaumik, M. Sujata, M.A. Venkataswamy, Fatigue failure of aircraft components, Engineering Failure Analysis, Volume 15, Issue 6, 2008, Pages 675-694, ISSN 1350-6307, https://doi.org/10.1016/j.engfailanal.2007.10.001. (https://www.sciencedirect.com/science/article/pii/S1350630707001409)
NIST Advanced Manufacturing Series 100-16 Literature Review of Metal Additive Manufacturing Defects Felix H. Kim Shawn P. Moylan Engineering Laboratory May 2018

## Slide 15: The statistical analysis involves (1) building a model
Y = Response
X = Defect Size (a)
  Hit/Miss
  Signal-Response
Logistic Regression
Linear Regression

## Slide 16: The statistical analysis involves (2) converting it to probability of detection (POD)
Probability of Detection Curve
X = Defect Size (a)
Probability of Detection
  Hit/Miss
  Signal-Response
Probability of Detection Curve

## Slide 17: (3) Estimate a 95% confidence interval on the probability curve.
Probability of Detection Curve
95% Confidence Interval Curve
a90
  Hit/Miss
  Signal-Response
Probability of Detection Curve
95% Confidence Interval Curve
90% Probability of Detection
a90/95
a90
a90/95

## Slide 18: Probability of Detection Studies inform Risk Calculations
FLIGHT HOURS
0 600 1200
=NDI Capability Limit
=Critical Flaw Size (Part Failure)
=Initial Flaw Size
RISK OF FAILURE
Initial Inspection
In-service Inspections
Flaw Growth Curve
Probability of Detection Curve
95% Confidence Interval Curve
90% Probability of Detection
a90/95
a90

## Slide 19: Agenda
Background
Statistical Analysis
Designing the Experiment
Example: XCT for AM

## Slide 20: Example: Additive Manufacturing: Opportunities and Challenges
CLSM
MPSS
XCT
CAD
Specimen Creation
Data Acquisition
MPSS – Mechanical Polishing Serial Sectioning
XCT – X-ray Computed Tomography
CLSM – Confocal Laser Scanning Microscopy
Data Processing
Segmentation (within dataset)
Reliability Assessment
Feature Matching (between datasets)
Registration (between datasets)
Detection & Sizing Statistics
Physics Modeling
Experimentation
Modeling & Simulation
Statistical Simulation
Automated Mechanical Polishing Serial Sectioning (Ground Truth)
Xray Computed Tomography Systems
 | Flaw Detected | No Flaw Detected
Flaw Exists | True Positive | False Negative
No Flaw Exists | False Positive | True Negative
XCT Data
MPSS Data
In-situ monitoring during printing

## Slide 21: Example: Additive Manufacturing: Opportunities and Challenges
Specimen Creation
MPSS – Mechanical Polishing Serial Sectioning
XCT – X-ray Computed Tomography
CLSM – Confocal Laser Scanning Microscopy
Physics Modeling
Experimentation
Modeling & Simulation
Statistical Simulation
In-situ monitoring during printing
CAD Modeled Part with designs for printed and machined features
(Right) Printed part after machining. (Left) Printed cap used to make features appear internal

## Slide 22: Example: Additive Manufacturing: Opportunities and Challenges
Specimen Creation
MPSS – Mechanical Polishing Serial Sectioning
XCT – X-ray Computed Tomography
CLSM – Confocal Laser Scanning Microscopy
Physics Modeling
Experimentation
Modeling & Simulation
Statistical Simulation
In-situ monitoring during printing

## Slide 23: Example: Additive Manufacturing: Opportunities and Challenges
CLSM
MPSS
XCT
CAD
Specimen Creation
Data Acquisition
MPSS – Mechanical Polishing Serial Sectioning
XCT – X-ray Computed Tomography
CLSM – Confocal Laser Scanning Microscopy
Physics Modeling
Experimentation
Modeling & Simulation
Statistical Simulation
Automated Mechanical Polishing Serial Sectioning (Ground Truth)
Xray Computed Tomography Systems
In-situ monitoring during printing

## Slide 24: Example: Additive Manufacturing: Opportunities and Challenges
CLSM
MPSS
XCT
CAD
Specimen Creation
Data Acquisition
MPSS – Mechanical Polishing Serial Sectioning
XCT – X-ray Computed Tomography
CLSM – Confocal Laser Scanning Microscopy
Physics Modeling
Experimentation
Modeling & Simulation
Statistical Simulation
Automated Mechanical Polishing Serial Sectioning (Ground Truth)
Xray Computed Tomography Systems
In-situ monitoring during printing

## Slide 25: Example: Additive Manufacturing: Opportunities and Challenges
MPSS – Mechanical Polishing Serial Sectioning
XCT – X-ray Computed Tomography
CLSM – Confocal Laser Scanning Microscopy
Data Processing
Segmentation (within dataset)
Feature Matching (between datasets)
Registration (between datasets)
Physics Modeling
Experimentation
Modeling & Simulation
Statistical Simulation
XCT Data
MPSS Data

## Slide 26: Example: Additive Manufacturing: Opportunities and Challenges
CLSM
MPSS
XCT
CAD
Specimen Creation
Data Acquisition
MPSS – Mechanical Polishing Serial Sectioning
XCT – X-ray Computed Tomography
CLSM – Confocal Laser Scanning Microscopy
Data Processing
Segmentation (within dataset)
Reliability Assessment
Feature Matching (between datasets)
Registration (between datasets)
Detection & Sizing Statistics
Physics Modeling
Experimentation
Modeling & Simulation
Statistical Simulation
Automated Mechanical Polishing Serial Sectioning (Ground Truth)
Xray Computed Tomography Systems
XCT Data
MPSS Data
In-situ monitoring during printing

## Slide 27: Example: Additive Manufacturing: Opportunities and Challenges
MPSS – Mechanical Polishing Serial Sectioning
XCT – X-ray Computed Tomography
CLSM – Confocal Laser Scanning Microscopy
Detection & Sizing Statistics
Physics Modeling
Experimentation
Modeling & Simulation
Statistical Simulation
XCT Equivalent Spherical Diameter
MPSS Equivalent Spherical Diameter (“Truth”)
Reliability Assessment

## Slide 28: Agenda
Background
Statistical Analysis
Designing the Experiment
Example: XCT for AM

## Slide 29: Questions?
Background
Statistical Analysis
Designing the Experiment
Example: XCT for AM
Opportunities for faculty and students to partner with us:
https://afresearchlab.com/careers-and-opportunities/students-and-faculty/#intern-box
Christine.Knott.1@us.af.mil

## Slide 30: References
Military Handbooks:
[67] U.S., Department of Defense. “MIL-STD-1530D”. Aircraft Structural Integrity Program, Airplane Requirements.
[69] U.S., Department of Defense. “MIL-HDBK-1823A”. Nondestructive Evaluation System Reliability Assessment, Department of Defense Handbook, August 2010
Educational Texts
[1] Agresti, A. Categorical Data Analysis. Wiley, Hoboken, New Jersey, 2nd edition, 2002.
[19] Casella, G. and R. Berger. Statistical Inference. Cengage Learning, Boston, Massachusetts, 2nd edition, 2001
[29] Hahn, G. and W. Meeker. Statistical Intervals. John Wiley and Sons, New York, New York, 1991.
[35] James, Gareth, Daniela Witten, Trevor Hastie, and Robert Tibshirani. An Introduction to Statistical Learning with Applications in R. Springer, New York, 2013.
[45] Kutner, M.H., C.I. Nachtsheim, J. Neter, and W. Li. Applied Linear Statistical Models. McGraw-Hill/Irwin, New York, New York, 5th edition, 2004.
[50] Meeker, W.Q. and L.A. Escobar. Statistical Methods for Reliability Data. Wiley, Hoboken, New Jersey, 1998.
[51] Montgomery, Douglas C. Design and Analysis of Experiments. John Wiley, New York, 9th edition, 2017.

## Slide 31: References: Selected Papers
[5] Annis, Charles, John C. Aldrin, and Harold A. Sabbagh. “NDT Capability”. Materials Evaluation, 44–54, January 2015.
[9] Berens, A.P. “NDE Reliability Data Analysis”. ASM Handbook, Vol. 17, Ed. 9, 689–701, 1989. [
[10] Berens, A.P. Probability of Detection (POD) Analysis for the Advanced Retirement for Cause (RFC)/Engine Structural Integrity Program (ENSIP) Nondestructive Evaluation (NDE) System Development, Technical Report AFRL-ML-WP-TR-2001-4010,. Technical report, Air Force Research Laboratory, 2000.
[11] Berens, A.P. and P.W. Hovey. “Statistical Methods for Estimating Crack Detection Probabilities”. ASTM STP 798: Probabilistic Fracture Mechanics and Fatigue Methods, 79–94, 1983.
[12] Berens, A.P. and P.W. Hovey. Flaw Detection Reliability Criteria. Technical Report AFWALTR-84-4022, Air Force Wright Aeronautical Laboratories, 1984.
[13] Berens, A.P. and P.W. Hovey. Flaw Detection Reliability Criteria Vol. I: Methods and Results. Technical Report AFWAL-TR-83-4089, Vol. 1, Air Force Wright Aeronautical Laboratories, 1984.
[14] Berens, A.P. and P.W. Hovey. “Quantifying NDI Capability for Damage Tolerance Analyses”. Review of Progress in Quantitative Nondestructive Evaluation, 1984.
[15] Berens, A.P. and P.W. Hovey. “The Sample Size and Flaw Size Effects in NDI Reliability Experiments”. Review of Progress in Quantitative Nondestructive Evaluation, 4:1327–1334, 1985.
[16] Berens, A.P. and P.W. Hovey. “NDE Reliability Data Analysis, Metals Handbook, Vol. 17, 9e, NDE and QC”. ASM International, 689–701, 1988.
[17] Berens, A.P. and P.W. Hovey. The Effect of Inspection Uncertainty on Crack Growth Based Maintenance Scheduling, Summary Paper. Technical Report Contract F33615-80C-5140, Air Force Materials Laboratory, February 1982.
[23] Gandossi, L. and C. Annis. “ENIQ report No. 41: Probability of Detection Curves: Statistical Best-Practices”. EUR – Scientific and Technical Research Series – ISSN1018-5593, ISBN 978-92-79-16105-6, 2010.
[24] Gandossi, L. and C. Annis. “ENIQ report No. 47: Influence of Sample Size and Other Factors on Hit/Miss Probability of Detection Curves”. EUR – Scientific and Technical Research Series – ISSN 1831-9424, ISBN 978-92-79-23018-9, 2010.
[30] Harding, C.A. and G.R. Hugo. “Experimental Determination of the Probability of Detection Hit/Miss Data for Small Data Sets”. Review of Progress in Quantitative Nondestructive Evaluation, 22:1823–1844, 2003
[34] Information, Aerospace Structures and Analysis Center. “The History of the Aircraft Structural Integrity Program”. Report No. 680.1B, June 1980.
[40] Knopp, J.S. and L. Zeng. “Statistical Analysis of Hit/Miss Data”. Materials Evaluation, Vol. 71, No. 3, 323–329, 2013
[54] Olin, B.D. and W.Q. Meeker. “Applications of Statistical Methods to Nondestructive Evaluation”. Technometrics, 38:95–112, 1996.
[55] P. Berens, Alan and Peter Hovey. “Evaluation of NDE Reliability Characterization. Volume I”. Air Force Wright Aeronautical Laboratories, 98, 12 1981.
[61] Singh, R. Three Decades of NDI Reliability Assessment. Technical Report Karta-3510-99-01, AF NDI Office, 2000.

## Slide 32: Backup Slides

## Slide 33: Hit/Miss Data has a Categorical Response: Logistic Regression
Inspector Call
Detection = Hit
No Detection = Miss
Hit/Miss
X = Defect Size (a)
Probability of Detection Curve
Modern methods encourage the use of:
- Firth’s Bias Adjusted Model (for separated classes) - Nonparametric Ranked Set Resampling Method (for very small sample sizes)
Notes: S.K. Bhaumik, M. Sujata, M.A. Venkataswamy, Fatigue failure of aircraft components, Engineering Failure Analysis, Volume 15, Issue 6, 2008, Pages 675-694, ISSN 1350-6307, https://doi.org/10.1016/j.engfailanal.2007.10.001. (https://www.sciencedirect.com/science/article/pii/S1350630707001409)
NIST Advanced Manufacturing Series 100-16 Literature Review of Metal Additive Manufacturing Defects Felix H. Kim Shawn P. Moylan Engineering Laboratory May 2018

## Slide 34: Hit/Miss Data has a Categorical Response: Logistic Regression
Inspector Call
Detection = Hit
No Detection = Miss
Hit/Miss
X = Defect Size (a)
a90
Probability of Detection Curve
95% Confidence Interval Curve
a90
a90/95
Legacy methods used Wald Confidence Intervals
Modern methods used Profile Likelihood Ratio Confidence Intervals
Notes: S.K. Bhaumik, M. Sujata, M.A. Venkataswamy, Fatigue failure of aircraft components, Engineering Failure Analysis, Volume 15, Issue 6, 2008, Pages 675-694, ISSN 1350-6307, https://doi.org/10.1016/j.engfailanal.2007.10.001. (https://www.sciencedirect.com/science/article/pii/S1350630707001409)
NIST Advanced Manufacturing Series 100-16 Literature Review of Metal Additive Manufacturing Defects Felix H. Kim Shawn P. Moylan Engineering Laboratory May 2018

## Slide 35: POD for Continuous-Response Data
Y = Response
X = Defect Size (a)
Signal-Response
Y = Response
X = Defect Size (a)
  Signal-Response
Notes: S.K. Bhaumik, M. Sujata, M.A. Venkataswamy, Fatigue failure of aircraft components, Engineering Failure Analysis, Volume 15, Issue 6, 2008, Pages 675-694, ISSN 1350-6307, https://doi.org/10.1016/j.engfailanal.2007.10.001. (https://www.sciencedirect.com/science/article/pii/S1350630707001409)
NIST Advanced Manufacturing Series 100-16 Literature Review of Metal Additive Manufacturing Defects Felix H. Kim Shawn P. Moylan Engineering Laboratory May 2018

## Slide 36: What are the assumptions of a linear model?
    Box Cox Transformation of Y:
      where is positive
    Transformation of : ()
Censoring
Truncation
Why are we using a simple Linear Regression?
Build a model relating NDI sensor response to crack size.
Transform model to a probability (of detection) curve.
Estimate a 95% confidence interval on the probability curve.

## Slide 37: 2. Transform model to a probability (of detection) curve.
If is distributed as a Standard Normal.
The cumulative distribution function of is the Probability of Detection Curve.
To get the values on the curve, just solve for a.
Probability of Detection Curve
X = Defect Size (a)
Probability of Detection
  Signal-Response
Y = Response
X = Defect Size (a)
  Signal-Response

## Slide 38: 3. Estimate a 95% confidence interval on the probability curve.
Probability of Detection Curve
95% Confidence Interval Curve
90% Probability of Detection
a90/95
a90
X = Defect Size (a)
Probability of Detection
  Signal-Response
We have the variance-covariance matrix of the linear model
?
We need the variance-covariance matrix of the POD Curve

## Slide 39: 3. Estimate a 95% confidence interval on the probability curve.
Delta Method
Given a differentiable function, , and a random variable such that ,
We have the variance-covariance matrix of the linear model
We need the variance-covariance matrix of the POD Curve
Derivatives describe how change

## Slide 40: 3. Estimate a 95% confidence interval on the probability curve.
Probability of Detection Curve
95% Confidence Interval Curve
90% Probability of Detection
a90/95
a90
X = Defect Size (a)
Probability of Detection
Wald Confidence Intervals are okay since we assumed Normality

## Slide 41: Research Questions for Reliability of NDI
NDI research is largely engineers doing their best to use statistics, without formal training
Under-conservative
Over-conservative
Models may be too simple
Observations may be dependent
a90/95???
a90
  Estimates may not exist
  Estimates may be biased
  Current models have strong assumptions
Methods only consider one NDE source
  Sample size may be too small
Sample Size
Confidence Interval Width/2
Low Freq EC

## Slide 42: Simulation of 252,000 hit/miss data sets which vary over important factors
⇝ Sample Size
⇝Distribution
N=35
N=120
NEW! Models
NEW! Confidence Intervals
Logistic Regression
Firth’s Bias Adjusted Model
The Lasso
Nonparametric Ranked Set Sampling
Standard Wald
Modified Wald
Modified Profile Likelihood Ratio
Profile Likelihood Ratio

## Slide 43: Confidence interval width is related to sample size and can cause over-conservatism
N=35
N=120
a90
a90/95
a90
a90/95

## Slide 44: Confidence interval width is related to sample size and can cause over-conservatism
Small sample → over-conservative
Larger sample → zero bias

## Slide 45: What are some examples of a too-simple model?
Flaw size is not 1D
NDE Response
Flaw Size

## Slide 46: Missing variables can decrease the quality of the fit.
Important variables are not included
NDE Response
Flaw Size
Hole Numbers
Materials
Layers
Notches vs Cracks
NDE Scanner Number
Gain/Calibration
Which model is better?
AICc and BIC
Likelihood Ratio Tests

## Slide 47: Many variables may be necessary, leading to complicated models
Explanatory Variables
  3 Materials (A, B, C)
  4 Layers, scanned 1 at a time
    Material above scanned layer
    Material below scanned layer – Material A below is significant
  6 Bolt Holes
  Crack locations – corners
  2 Crack types
    Fatigue cracks
    EDM notches
  Crack Lengths (continuous values)
Signal Response
  Percent screen height (0% to 100%)
Interaction between crack size, material C and EDM notches

## Slide 48: Missing variables can decrease the quality of the fit and change the estimates of a90 and a90/95

## Slide 49: How do you handle dependent observations for POD?
Sensor-Crack Pair 1
Sensor-Crack Pair 2
…
Sensor-Crack Pair 60
Time
Time
Noise Signal
Crack Signal
ydec = Detection Threshold
Independent POD uses a linear model with
Dependent POD uses a linear mixed model with
scalar
matrix

## Slide 50: What structure should the variance matrix have?
between groups
within
groups
AR(1): Equally-spaced
SPOW: Un-equally-spaced
Open question: How would you model the data when you also have spatial correlation?
Sensors
Crack
Specimen

## Slide 51: Different models yield different estimates; assuming independence is under-conservative
Assume independence
Between + Within
1
9
13
21
25
17
5
Naïve (Independent) Models
CS Mixed Model (Improved)
AR(1) Mixed Model
Reliably Detectable Flaw Size

## Slide 52: What could go wrong with a POD study? Estimates do not exist
a90/95???
a90

## Slide 53: Existence can be compared between new modeling types and new confidence intervals
MODELS
CONFIDENCE INTERVALS
High Risk
Low Risk

## Slide 54: For small samples, Wald confidence intervals have more over-conservative bias than profile likelihood methods
Over-conservative (Bias > 0):
  Inspect more often than necessary
Unbiased (Bias = 0)
  Inspect when needed
Under-conservative (Bias < 0):
  Not enough inspections

## Slide 55: Smaller sample sizes have more bias, across modeling types
Over-conservative (Bias > 0):
  Inspect more often than necessary
Unbiased (Bias = 0)
  Inspect when needed
Under-conservative (Bias < 0):
  Not enough inspections

## Slide 56: Smaller sample sizes have more bias, across modeling types
Over-conservative (Bias > 0):
  Inspect more often than necessary
Unbiased (Bias = 0)
  Inspect when needed
Under-conservative (Bias < 0):
  Not enough inspections

## Slide 57: What are the assumptions of a linear regression model?
Residuals =
Pearson Standardized Residuals
Linear in the parameters
Random errors ( are identically and independently distributed Gaussians
Normality Test of Residuals
Durbin-Watson Test for Autocorrelation
Constant Variance Test

## Slide 58: What are the assumptions of a linear regression model?
Residuals =
Pearson Standardized Residuals
Linear in the parameters
Random errors ( are identically and independently distributed Gaussians
Normality Test of Residuals
Durbin-Watson Test for Autocorrelation
Constant Variance Test

## Slide 59: What are the assumptions of a linear regression model?
Residuals =
Pearson Standardized Residuals
Linear in the parameters
Random errors ( are identically and independently distributed Gaussians
Normality Test of Residuals
Durbin-Watson Test for Autocorrelation
Constant Variance Test

## Slide 60: Censored and Truncated Data